## Slide 1: Removal of Excess Gaseous and Aqueous Sulfide from Vertical Flow Bioreactor Effluent Using Activated Carbon and Solar-Powered Blowers
Robert W. Nairn
David L. Boren Distinguished Professor
Viersen Presidential Professor
Taylor Wall
Graduate Research Assistant

## Slide 2
Problems/Challenges
System Design
Conclusions
System Performance

## Slide 3
Problems/Challenges

## Slide 4
Tar Creek Superfund Site
National Priorities List (1983)
Elevated Fe, Zn, Cd, Pb, As in water, chat, soils and biota
Mining “mega-site”
Ten Native American Tribes
OU CREW comprehensive watershed monitoring
1997 - present
Streams, point (artesian discharges), nonpoint (waste pile runoff / leachate) sources
KS
OK

## Slide 5
Tar Creek Superfund Site
National Priorities List (1983)
Elevated Fe, Zn, Cd, Pb, As in water, chat, soils and biota
Mining “mega-site”
Ten Native American Tribes
OU CREW comprehensive watershed monitoring
1997 - present
Streams, point (artesian discharges), nonpoint (waste pile runoff / leachate) sources
Tar Creek
Beaver Creek
Lytle Creek
Elm Creek
Unnamed Tributary
KS
OK

## Slide 7: Tar Creek Operable Unit 1 Surface and Ground Water Decision
Initial artesian discharges (1979)
USEPA concluded that (1984):
“impacts to (surface waters) are due to irreversible man-made damages resulting from past mining operations at the site”
Fund-balancing waiver used
  Costs prohibitively high to address surface water contamination
Unabated flows for nearly 40 years

## Slide 8: Center for Restoration of Ecosystems and Watersheds
Watershed biogeochemistry
  Drainage-basin scale evaluations
  Materials and energy transport and fate
Ecological engineering
  Water and land reclamation
  Ecosystem remediation, restoration and creation
  Passive treatment systems
  Low impact development
  Water reuse

## Slide 9: CREW builds ecosystems
Watershed biogeochemistry
  Drainage-basin scale evaluations
  Materials and energy transport and fate
Ecological engineering
  Water and land reclamation
  Ecosystem remediation, restoration and creation
  Passive treatment systems
  Low impact development
  Water reuse

## Slide 10
Mayer Ranch PTS
Hartshorne PTS
Red Oak PTS
Southeast Commerce PTS
Gowen PTS
Leboskey PTS

## Slide 11
Mayer Ranch PTS
Hartshorne PTS
Red Oak PTS
Southeast Commerce PTS
Gowen PTS
Leboskey PTS

## Slide 12: Bacterial sulfate reduction in Vertical Flow Bioreactors (VFBRs)
Notes: Organic matter oxidized, sulfate reduced to sulfide

## Slide 13: Bacterial sulfate reduction in Vertical Flow Bioreactors (VFBRs)
SO42- + 2CH2O  H2S + 2HCO3-
H2S + Zn2+ + 2HCO3-  ZnS(s) + 2H2O + 2CO2
Notes: Organic matter oxidized, sulfate reduced to sulfide

## Slide 14: Bacterial sulfate reduction in Vertical Flow Bioreactors (VFBRs)
SO42- + 2CH2O  H2S + 2HCO3-
H2S + Zn2+ + 2HCO3-  ZnS(s) + 2H2O + 2CO2
Design for ~20 year lifetime
Potential excess sulfide production
Notes: Organic matter oxidized, sulfate reduced to sulfide

## Slide 15: Excess Sulfide Concerns
Corrosive, poisonous and flammable
Aqueous sulfide
  Potential nuisance constituent
  Toxic to aquatic life > 0.002 mg/L (USEPA 1986)
Gaseous sulfide
  Nuisance odor problems
  Substantial human health effects

## Slide 16: Excess Sulfide Concerns
Gaseous H2S (ppmv) | Symptoms/Effects
0.00011-0.00033 | Typical background concentrations
0.01-1.5 | Odor threshold
2-5 | Nausea, headache, loss of sleep
20 | Fatigue, loss of appetite, headache, irritability, poor memory, dizziness
50-100 | Conjunctivitis, respiratory tract irritation, digestive upset, loss of appetite
100-150 | Olfactory fatigue and paralysis (loss of sense of smell)
200-300 | Pulmonary edema from prolonged exposure
500-700 | Staggering, collapse in 5 minutes, damage to eyes in 30 minutes
700-1000 | Rapid unconsciousness, "knockdown" or immediate collapse within 1 to 2 breaths, breathing stops, death within minutes
1000-2000 | Nearly instant death

## Slide 17: Excess Sulfide Concerns
Gaseous H2S (ppmv) | Symptoms/Effects
0.00011-0.00033 | Typical background concentrations
0.01-1.5 | Odor threshold
2-5 | Nausea, headache, loss of sleep
20 | Fatigue, loss of appetite, headache, irritability, poor memory, dizziness
50-100 | Conjunctivitis, respiratory tract irritation, digestive upset, loss of appetite
100-150 | Olfactory fatigue and paralysis (loss of sense of smell)
200-300 | Pulmonary edema from prolonged exposure
500-700 | Staggering, collapse in 5 minutes, damage to eyes in 30 minutes
700-1000 | Rapid unconsciousness, "knockdown" or immediate collapse within 1 to 2 breaths, breathing stops, death within minutes
1000-2000 | Nearly instant death
OSHA PELs
8-hour: 10 ppmv
Ceiling: 20 ppmv
NIOSH IDLH: 100 ppmv

## Slide 18: Excess Sulfide Production – Mayer Ranch PTS
Chart: Aqueous Sulfide (mg/L)
| Inflow | OX out | SF out | VF out | RA out | LB out | PW out
Fall 2010 | 0.25 | 0.25 | 0.25 | 4.8886 | 0.38833 | 0.25 | 0.25
Spring 2011 | 0.25 | 0.25 | 0.25 | 4.6103 | 0.26405 | 0.25 | 0.25
Summer 2011 | 0.25 | 0.25 | 0.25 | 27.0566 | 16.4798 | 16.9423 | 2.363
Excess aqueous sulfide
Continuous operation since 2008
First PTS in TSMD

## Slide 19
System Design

## Slide 20
Southeast Commerce Site

## Slide 21: Southeast Commerce
“Red Hole” and “Green Hole” collapse features
Water discharges into Unnamed Tributary to Tar Creek
Collapses filled and surface reclaimed 2006
Commerce, OK
US66
Unnamed tributary

## Slide 22: Southeast Commerce
“Red Hole” and “Green Hole” collapse features
Water discharges into Unnamed Tributary to Tar Creek
Collapses filled and surface reclaimed 2006
Mine water collected in French Drain and directed to UT
Mayer Ranch Passive Treatment System
Commerce, OK
US66
Unnamed tributary
Stormwater pond
Commerce High School and Sports Complex
Mickey Mantle Memorial

## Slide 23: Southeast Commerce
“Red Hole” and “Green Hole” collapse features
Water discharges into Unnamed Tributary to Tar Creek
Collapses filled and surface reclaimed 2006
Mine water collected in French Drain and directed to UT
Mayer Ranch Passive Treatment System
Commerce, OK
US66
Unnamed tributary
Stormwater pond
Commerce High School and Sports Complex
Mickey Mantle Memorial
Untreated SEC Waters | 
pH | 6.06
T. Alk. | 350 mg/L CaCO3
Fe | 138 mg/L
Zn | 6.2 mg/L
Ni | 0.52 mg/L
Cd | 20 mg/L
Pb | 80 mg/L
As | 38 mg/L
SO42- | 2100 mg/L
Q | 100 gpm

## Slide 24
Southeast Commerce Passive Treatment System
Ecological engineering field research site
Designed for 550 m3/d
Receives elevated Fe, Zn, Pb, Cd, As, SO4
Four total process units
Shared water surfaces/baffles/z-piling
Solar-powered aeration/reaeration
Limited operation/maintenance
Discharge meets receiving stream criteria
C4: Final polishing unit
Stormwater Pond
C3: Vertical flow bioreactor
C2: Surface flow wetland
C1: Oxidation pond
System start up 02/17
N in
S in
Up in
Oklahoma DEQ funding 2015-present
4 process units
  - Directional baffle curtains and z-piling
  - Innovative solar-powered air-lift aerators
  - Unique GAC S2-capture system
Second PTS in Tri-State Mining District
Continuous operation since 02/2017

## Slide 25
Southeast Commerce Passive Treatment System
Ecological engineering field research site
Designed for 550 m3/d
Receives elevated Fe, Zn, Pb, Cd, As, SO4
Four total process units
Shared water surfaces/baffles/z-piling
Solar-powered aeration/reaeration
Limited operation/maintenance
Discharge meets receiving stream criteria
C4: Final polishing unit
Stormwater Pond
C3: Vertical flow bioreactor
C2: Surface flow wetland
C1: Oxidation pond
System start up 02/17
N in
S in
Up in
Oklahoma DEQ funding 2015-present
4 process units
  - Directional baffle curtains and z-piling
  - Innovative solar-powered air-lift aerators
  - Unique GAC S2-capture system
Second PTS in Tri-State Mining District
Continuous operation since 02/2017

## Slide 26
VFBR Substrate
1,000 yd3 single- shredded wood chips
132 tons (~240 yd3) spent mushroom compost
~3.0 ft thickness
Underdrain 616 tons non-calcareous AASHTO #57 aggregate (~2.0 ft thickness)

## Slide 27: Custom-Designed Odor Control System
VFBR
Final Polishing Unit
Odor Control System
Four Cell VFBR Underdrain Effluent
Airline
GACF
Solar-powered exhaust blower in shed
Solar Array
Water
Air
3200-W solar photovoltaic array
1 regenerative vacuum blower
Granular activated carbon (GAC) S2- filter (ACF)
2 regenerative pressure blowers
Float-mix aerators

## Slide 29: Float-Mix Aerators
Two each in Oxidation Pond and Final Polishing Unit

## Slide 30
System Performance

## Slide 31: Water Quality Changes
 | Southeast Commerce | 
 | In (n=80) | Out (n=22)
pH | 6.06 | 7.02
AlkT (mg/L) | 350 | 117
FeT (mg/L) | 138 | 0.79
ZnT (mg/L) | 6.15 | 0.69
NiT (mg/L) | 0.52 | 0.06
CdT (mg/L) | 20 | <PQL
PbT (mg/L) | 80 | 26
AsT (mg/L) | 38 | <PQL
SO4-2 (mg/L) | 2100 | 1956
Q (GPM) | --- | 125

## Slide 32: Water Quality Changes
 | Southeast Commerce | 
 | In (n=80) | Out (n=22)
pH | 6.06 | 7.02
AlkT (mg/L) | 350 | 117
FeT (mg/L) | 138 | 0.79
ZnT (mg/L) | 6.15 | 0.69
NiT (mg/L) | 0.52 | 0.06
CdT (mg/L) | 20 | <PQL
PbT (mg/L) | 80 | 26
AsT (mg/L) | 38 | <PQL
SO4-2 (mg/L) | 2100 | 1956
Q (GPM) | --- | 125
OP
Fe and As ↓
27 g Fe m-2 d-1
VFBR
Zn, Ni, Cd, Pb ↓
0.6 mol SO4-2 m-3 d-1
FPU
O2↑
WL
Fe ↓

## Slide 33: System Aqueous Sulfate and Sulfide

## Slide 34
ACF Gaseous Sulfide

## Slide 35
ACF Temperature and Relative Humidity

## Slide 36
 | Air Flow (L/sec) | Temperature (°C) | Relative Humidity (%)
ACF Influent | 14±0.2 | 23±2.7 | 65±5.5
ACF Effluent | 15±0.1 | 31±9.1 | 38±1.5

## Slide 37
 | Air Flow (L/sec) | Temperature (°C) | Relative Humidity (%)
ACF Influent | 14±0.2 | 23±2.7 | 65±5.5
ACF Effluent | 15±0.1 | 31±9.1 | 38±1.5
2H2S + 4O2  2SO2 + 2H2O + O2  2H2SO4
Elevated gaseous sulfide under moist aerobic conditions forms sulfuric acid

## Slide 38: ACF media autopsy
~1.8 m
48 cm from top to media surface
0.9 m
0.9 m
PVC Pipe to Exhaust Blower
Condensate Drain
PVC Pipe to OCS
PVC Support Legs
Perforated HDPE Support Plate
136,000 mg S/kg
138,000 mg S/kg
132,000 mg S/kg
155,000 mg S/kg
248,000 mg S/kg
129,000 mg S/kg
October 2018
20 months operation
Core samples in lifts
Notes: Delete metals and showS with depth on schematic

## Slide 39: Sulfur mass balances
Missing 10%
ACF S Mass Balance

## Slide 40: Sulfur mass balances
Missing 10%
ACF S Mass Balance
VFBR S Mass Balance | kg S
Aqueous S retained - from water quality analyses | 1600
VFBR substrate S – from substrate analyses | 1100
S required for MeS precipitation | 640

## Slide 41
Irreversibly Damaged?
Pre-PTS
Post-PTS

## Slide 42
Receiving Stream Recovery

## Slide 43: Receiving Stream Recovery
Long-term water quality data collection (15+ years)
Long-term fish community analysis (12+ years)
Documented changes in water quality and ecological community
Tar Creek
Unnamed Tributary
UT-U
UT-R
UT-D
UT-P
UT-HS
2005
2009
2012

## Slide 44: Unnamed Tributary fish data
Catch per unit effort (CPUE) |  |  | 
Scientific name | Common name | 2005-07 | 2009-16
Gambusia affinis | Western mosquitofish | 39.24 | 187.60
Lepomis cyanellus | Green sunfish | 0.81 | 16.80
Lepomis macrochirus | Bluegill | 1.00 | 3.00
Lepomis megalotis | Longear sunfish | 0.02 | 6.80
Notemigonus crysoleucas | Golden shiner | 0.17 | 0.60
Lepomis gulosus | Warmouth | 0.07 | 1.0
Lepomis microlophus | Redear sunfish | 0 | 18.00
Lepomis sp. | Sunfish hybrid | 0 | 2.5
Labidesthes sicculus | Brook silversides | 0 | 2.0
Etheostoma gracile | Slough darter | 0 | 0.80
Ameiurus melas | Black bullhead | 0 | 0.40
Fundulus notatus | Blackstriped topminnow | 0 | 0.40
Pomoxis annularis | White crappie | 0 | 0.30
Micropterus salmoides | Largemouth bass | 0 | 0.20
 | Species richness | 6 | 14

## Slide 45
Conclusions

## Slide 46: Study Conclusions
VFBR bacterial sulfate reduction produced excess sulfide beyond that needed for trace metal precipitation
Capture and removal of gaseous sulfide helped to decrease aqueous sulfide concentrations
Solar-driven vacuum blower and an activated carbon filter (ACF) effectively removed gaseous sulfide
Solar-driven float mix aerators (FMAs) effectively removed aqueous sulfide in the final polishing unit (FPU)
Estimates of sulfur species in aqueous, gaseous and solid phases accounted for reasonable mass balance of sulfur
Notes: 640 kg S needed for complete trace metal precipitation, and we’re producing almost double that

## Slide 47: Big Picture Conclusions
Passive treatment is a demonstrated ecological engineering technology to improve mine water quality
Water quality improvement has direct influence on ecological metrics in stream and riparian areas
Widespread applicability requires revisiting and revising administrative and regulatory constraints

## Slide 48: Special Thanks
Buck Neely
Tim Danehy
Russ Dutnell

## Slide 49: Acknowledgements
Our private landowner
  Corbus family
Our funding sources
  ODEQ Land Protection Division
  Grand River Dam Authority Ecosystems Management
Our partners
  OU CREW, CEES and Biology
  Quapaw Nation of Oklahoma
  City of Commerce
  Northeastern Oklahoma A&M College
  CH2M-Hill team and subcontractors
  BioMost Inc. and Riverman Engineering
  LEAD Agency
CREW past and present

## Slide 50: The CREW
K Strevett, R Knox, W Matthews, J Basara, E Bergey, R Kolar, J LaBar, B Page, C Kellogg, A O’Sullivan, M Zhang, J Gu, J Halstead, F Walker, M Mercer, E Breetzke, C DuBois, R Garrett, V Arvidson, N Iverson, B Winter, D Athay, C Porter, J Coffey, T Traw, C Gause, R White, D Hensley, M Roberts, D Lutes, W Strosnider, A Garrido, C Neely, B Santamaria, A Brewer, W Andrews, J McAllister, A Smith, S Yepez, J Brumley, B Furneaux, M Rice, R Dutnell, J Arango, B Holzbauer-Schweitzer, L Oxenford, E Thornton, E Fielding, N Shepherd, A Sikora, D Nguyen, T Wall, N Berg-Mattson, M Dorman, Z Tang, J Ingendorf, H Stanfield, K Steele, A Marsh, T Verlander, G Huey, M Foster, M Bible, T Haviland, C Evenson, M Smith, A Spence, A Kirchner, E Trawinski, S Lipe, M Sprowls, C Cogburn, K Wahnee, E Spargo, D Miller, I Gray, K Swanson, W Katzenstein, E Solchick, M Brown, I Petterson, J Bennette, D Tepo, A Oberst, A Danielson, H Bragg, S Wong, A Donaldson, J Clifton, P Eger, B Winfrey, T Lenox, M McMahon, K Ryan, S McClenahan, W Runyon, L Mignogna, V Ferrufino, T Bisaner, Z Samson, V Nadeq, C Turley, S Guzman, S Zawrotny, J Fowler, D Herron, M Cousatte, Maguire, C Milligan, D Wright, C Iddings, D Bruer, K Markley, C Robb, T Pipher, S Hobson, E Wu, O Yancey, B Dittrich, D Morris, K Kauk, A Sutter, K Walker, D Ertugrul, C Cook, et al.

## Slide 51
Questions?
http://CREW.ou.edu nairn@ou.edu