## Slide 1: Source Control or How to Eliminate Acidophiles and Influence Water Quality
Paul Eger
Global Minerals Engineering / Linkan Engineering
Jim Gusek, Lee Josselyn
Linkan Engineering
Tom Clark
Solfatara Laboratories
Global Minerals Engineering
Notes: Thanks for including us in your program. My co-author, Jim Gusek and I have been involved with passively treating acid rock drainage for about 30 years and we came to the realization that source control of ARD might be more sustainable. I’d like to introduce you to some general concepts of source control and how these might be applied at

## Slide 2: Outline
What is source control?
Why is it important?
Study Site
Approach
Results
Conclusions
Next steps

## Slide 3: Acid Rock Drainage Tetrahedron
Fuel
Air
Heat
FIRE
Oxidizer
(Air, Fe+3)
Bacteria
Pyrite
Water
ARD
Notes: Before we get started, we need to understand that ARD formation is analogous to the combustion triangle we all learned in elementary school. Cut off the air, fuel or heat supplies and you won’t have a fire. (CLICK)
ARD formation is similar, you need pyrite (of course), air, water and not fully appreciated, bacteria: acidithiobacillus ferro-oxidans . Cut off one or more corners of the ARD tetrahedron, and ARD kinetics is greatly suppressed. But if you cut off the bacteria corner, you can slow the kinetics of ARD formation by 3 orders of magnitude (that’s a thousand times slower).

## Slide 4: Why is it Important?
IN PERPETUITY
Unless we can find practical
source control remedies
Notes: The mining industry suffers from a huge bacterial infection and acidithiobacillus ferro-oxidans is the main cause of this geological disease. Unless we figure out a remedy for the patient, we’re looking at PERPETUAL TREATMENT; in perpetuity is a long time. This is NOT a sustainable outcome.

## Slide 5
Bacteria
Water
Pyrite
Oxidizer
(Air, Fe+3)
DO NOTHING = PERPETUAL TREATMENT
DO SOMETHING (anything) = SUSTAINABLE REMEDIES
Acid Rock Drainage Tetrahedron
Notes: It’s not enough to kill the bad bacteria, just killing the bacteria leads to short term control

## Slide 6: Source Control Options
Pyrite
  Avoidance
  Processing
Water
  Covers
    Impermeable
    Evaporative
Oxidizer
  Subaqueous disposal
  Organic covers
Bacteria
  Bactericides
  Organic materials

## Slide 7: Why Bacteria?
They are everywhere!
Shown to greatly accelerate rate of pyrite oxidation
  Rate increases by orders of magnitude
Been found in circumneutral mine drainage
Major influence on the ultimate water quality
Acidithiobacillus Ferrooxidans

## Slide 8: Changing the Microbial Community
Eliminate with bactericide
    Surfactants – Sodium Lauryl Sulfate
    US Bureau of Mines 1980’s
    Create conditions for other bacteria
Change environment and replace by competition
    Organics – milk
    Western Research Institute ( 2008)
    Create biofilms

## Slide 9: THE SITE

## Slide 10: Barite Hill Gold Mine
McCormick, South Carolina
Historic mining 1850’s
Open pit mining 1991-1994
Reclamation from 1995 to 1999
Bankruptcy July 1999
Emergency action 2007
Superfund designation 2009
Notes: Produced 59,000 oz Au and 109,000 oz silver
Remaining bond $700,000

## Slide 11
Inventory Results 2007
10-acre acid pit lake pH 1.5 – 2.2
    No outlet
    Water level rising
Acid seeps from Leach Pad
Acid seeps from Spent Ore Landfill
Acid seeps from Waste Rock Pile
Ditches severely eroding

## Slide 12: Remedial Action

## Slide 13
Spillway Construction

## Slide 14
Lake Neutralization and Carbon Addition

## Slide 15
Stockpile reclamation

## Slide 16
2016
pH 2.5
Waste rock

## Slide 17: Problem
Pit water continued to be acidic with high levels of trace metals
Periodically retreated pit with sodium hydroxide
Immediate pH increase but slow decline
Continued input of acid from waste rock appears to be major source
Need a more permanent and sustainable solution

## Slide 18: Project Goal
Develop and conduct proof of principle tests to develop innovative remedial actions for the site

## Slide 19: Project Objectives
Collect and characterize representative samples from the site
Conduct initial screening tests to refine proof of principle testing
Conduct proof of principle testing for various site components
  Waste rock stockpiles
  Pit water
  Groundwater
  Pit bottom
Notes: Focus on waste rock stockpile since it appears to be major source of loads to the pit

## Slide 20: Proof of Principle
Objective was to determine only if the technique could work
Developed screening protocols to facilitate testing
  Based on standard testing techniques when possible
  Eliminate dead ends early
Amendments based on screening tests
    No optimization
To Go or NoT TO Go;
that is the question

## Slide 21: Sample Collection
Fine particles

## Slide 22: Sample Preparation
Sample contained large percentage of fines
  Poor flow properties
Agglomerated sample to improve hydraulic conductivity
  Agglomeration process only required distilled water
  Use this sample in all reactors
Notes: Discuss advantages and disadvantages

## Slide 23: Stockpile conceptual model

## Slide 24: Approach
Develop specific test condition to simulate each zone in the stockpile
  Unsaturated
  Transition
  Saturated
Screening Tests
  Beaker Tests (milk & surfactants)
  Modified US Bureau of Mines (surfactants)

## Slide 25: Unsaturated Zone
Portion of the stockpile
permanently above water
Aerobic environment
Reaction products moved by water infiltration
Contains both residual and sulfide acidity
Residual or stored acidity = reaction products that have not been rinsed out of stockpile
Sulfide or potential acidity = unreacted sulfide minerals which can react in the future

## Slide 26: Unsaturated Tests- Methods
Modified humidity cell test
  20 kg sample
  One week drying cycle
    Similar to standard humidity cells
  Peristaltic pump - flooded from bottom with distilled deionized water
  Water pumped out
10 kg charge
20 kg charge
Gravel layer not shown

## Slide 27: Unsaturated Tests- Treatments
Control
Sodium Lauryl Sulfate (SLS)/Alkalinity
Sodium Lauryl Sulfate (SLS)/Alkalinity/Milk
  Sequential application
Milk
Milk /Alkalinity
Bacterial inoculum added to milk reactors

## Slide 28: Unsaturated Zone 20-kg Test pH Results
Control
Milk
Milk/Alkalinity
SLS/Alkalinity
SLS/Alkalinity/Milk

## Slide 29: Unsaturated Zone 20-kg Test Microbial Suppression

## Slide 30: Transition Zone
Portion of the stockpile between high and low water level
Alternating wet and dry cycle
Ideal conditions for oxidation and transport

## Slide 31: Transition Zone Tests- Treatments
Control
Sodium Lauryl Sulfate (SLS)/Alkalinity
Milk
Milk /Alkalinity

## Slide 32: Transition Tests- Methods
  20 kg sample
  Alternate one week cycles flood and dry
  Reactors flooded from bottom with peristaltic pump
  Simulated natural groundwater was used as rinse
  Water pumped out

## Slide 33: Transition Zone 20-kg Test pH Results
SLS/Alkalinity
Milk/Alkalinity
Milk
Control

## Slide 34: Transition Zone – Microbial Results

## Slide 35: Transition Zone – Microbial Results
Week 9
Week11
Notes: Commercial heap leaches10 6 to 10 8
Sampled ½ way through draw down to minimize contamination

## Slide 36: Saturated Zone
Portion of the stockpile below low water level
Permanently flooded
Low pH
High ferric iron
Sulfide oxidation occurs due to ferric iron

## Slide 37: Saturated Zone Tests- Treatments
Alkalinity
Milk /Alkalinity
Since primary oxidation is by ferric iron
SLS would not be expected to be effective

## Slide 38: Saturated Zone Tests - Methods
  20 kg sample
  Permanently flooded
  Sample volume withdrawn weekly
  Water replaced
  Amendments added over time
      Initial portion of study
    Simulate groundwater flow

## Slide 39: Saturated Zone-pH results
Milk/Alkalinity
Alkalinity

## Slide 40: Saturated Zone-Microbial results
Alkalinity
Milk/Alkalinity
Week 9
Week 11

## Slide 41: Conclusions
Source Control Works!

## Slide 42: Conclusions
Microbial community successfully modified
SLS/ Alkalinity effective at suppressing acidophilic bacteria in the unsaturated and transition zone conditions
Milk/Alkalinity
  Effective in transition and saturated zone
  Neutralized acidity
  Replaced acidophiles with sulfate reducers

## Slide 43: Next Steps
Phase 2
  Refine site model
    Mass release estimates
  Determine optimum addition rates
  Application methods
    Drip irrigation
    Wells
    Trenches
Field Testing
Shallow Wells/Trench

## Slide 44: Acknowledgements
  Candice Teichert, US EPA
  Reginald G. Dawkins, Black and Veatch Special Projects
  Joel Padgett, South Carolina, DHEC

## Slide 45: The Choice
IN PERPETUITY
Innovation Works!
Quest
ions
?
Notes: The mining industry suffers from a huge bacterial infection and acidithiobacillus ferro-oxidans is the main cause of this geological disease. Unless we figure out a remedy for the patient, we’re looking at PERPETUAL TREATMENT; in perpetuity is a long time. This is NOT a sustainable outcome.