## Slide 1: SORPTION OF METALS FROM WATER BODIES POLLUTED BY MINING AND REUSE OF HYDROCHAR IN LAND RECLAMATION
PRESENTED BY: BENJAMIN QUARDEY
COMMITTEE: PROFS. NATALIE KRUSE DANIELS, SARAH DAVIS, LEI WU
ASRS CONFERENCE 2022
MASTER OF SCEINCE IN ENVIRONMENTAL STUDIES (MSES)
OHIO UNIVERSITY ASRS 39TH ANNUAL CONFERENCE

## Slide 2: INTRODUCTION
Acidic or alkaline drainage with high metals concentrations.
Mine water is the largest anthropogenetic activity associated with mining activity.
Single largest impediment to surface water and groundwater.
Large negative impacts on aquatic ecosystems.

## Slide 3: ADSORPTION PARAMETERS OF HYDROCHAR
Table 1: hydrochar parameters
ND-not detected, NM-not measured, NS-not specified, N- negligible

## Slide 4: HYDROCHAR PRODUCTION
Fig 3.Hydrochar Production model

## Slide 5: SORPTION MECHANISM
ION EXCHANGE: Hydrochar sample and heavy metals being examined exchange protons and ionized cations with dissolved salts.
ELECTROSTATIC ATTRACTION: Hydrochar sample interacts chemically by ion exchange with the heavy metals via the negative charge on the hydrochar surface.
SURFACE COMPLEXATION: Multi atom forms metal ligands forming oxygen and carboxyl bond with specific heavy metals.
Fig. 4. Sorption mechanism

## Slide 6: OBJECTIVES
MAIN OBJECTIVE
SPECIFIC OBJECTIVES
Determine the capacity of hydrochar produced from anaerobic digestate for removing heavy metals (copper, cadmium, zinc) in mine water.
Study the adsorption kinetic of hydrochar at different reaction times.
Assess reuse of hydrochar for land amendment.
Test the capacity of hydrochar for sorption of metals.

## Slide 7: METHODOLOGY
Preparation of synthetic mine water solution
Sorption capacity and contact ratio
Sorption kinetic test
Desorption test

## Slide 8: VOLUMES AND CONCETRATIONS
Stock solution | Concentrations (mg/L) | Volumes (mL) | Target concentrations mg/L
Zn | 65.38 | 1.53 | 10
Cu | 63.55 | 3.93 | 10
Cd | 112.41 | 13.71 | 3
Fig 6: synthetic mine water
Table 1: Concentrations of target metals

## Slide 9: HYDROCHAR SAMPLES
A
B
C
Fig 4: A, B and C are hydrochar samples 180 , 220 , and 260 respectively derived from anaerobic
digestate produced at the Florida Institute of Technology.

## Slide 10: SORPTION CAPACITY
 |  | pH 4 |  |  | pH 7 |  | 
0.5 g | 1 g | 2 g | W/H | 0.5 g | 1 g | 2 g | W/H
5 g | 8 g | 10 g | Ctrl | 5 g | 8 g | 2 g | Ctrl
Table 2: triplicates of hydrochar samples

## Slide 11: SORPTION CAPACITY
50 mL centrifuge tubes containing 35 mL of synthetic neutral mine water or synthetic acidic mine water.
The solution was mixed with hydrochar at 150 rpm on a shaker plate for 24 hours.
A 0.45 µm filter paper after the incubation period was used for filtration.
The effluent was analyzed using the ICP-OES for target metal concentration.
Fig 7: hydrochar sample after incubation period

## Slide 12: RESULTS REMOVAL RATES
Fig 7: 180 hydrochar sample for pH 4
Fig 8: 180 hydrochar sample for pH 7
Chart: Removal rate pH 4
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Metal removal rate Cd (%) | 10.7413 | 13.9561 | 14.3343 | 41.5658 | 63.3132 | 76.1725 | -1.9289
Metal removal rate Cu (%) | 15.9451 | 4.8546 | 2.5197 | 15.8478 | 19.0583 | 18.8637 | 17.4044
Metal removal rate Zn (%) | 6.0064 | 10.1701 | 9.107 | 31.5202 | 42.0624 | 48.4408 | -5.3331
Chart: Removal rate pH 7
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Metal removal rate Cd (%) | 21.4848 | 26.8841 | 16.9854 | 37.6828 | 61.7548 | 72.1035 | 15.1856
Metal removal rate Cu (%) | 91.6972 | 33.3333 | 17.094 | 41.1477 | 3.4188 | -1.7094 | 99.8779
Metal removal rate Zn (%) | 18.7175 | 19.7961 | 16.0702 | 29.5029 | 32.3463 | 45.6809 | 18.9136

## Slide 13: RESULTS SORPTION CAPACITY
Fig 10: 180 hydrochar sample for pH 7
Fig 9: 180 hydrochar sample for pH 4
Chart: Sorption capacity pH 4
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Sorption Capacity Cd (mg/L) | -0.25109 | -21.235 | -10.4805 | -0.0013139 | 1.8153 | 2.3838
Sorption Capacity Cu (mg/L) | 10.6896 | 0.8646 | -0.0393 | 1.0611 | 0.8253 | 0.65238
Sorption Capacity Zn (mg/L) | -1.8666 | -0.2142 | -0.1989 | 0.69462 | 0.66173 | 0.63954
Chart: Sorption Capacity pH 7
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Sorption Capacity Cd (mg/L) | -13.426 | -3.425 | -4.7265 | 0.6302 | 2.2262 | 2.4112
Sorption Capacity Cu (mg/L) | 73.2552 | 17.8422 | 6.3076 | 4.0715 | 1.0267 | 0.65631
Sorption Capacity Zn (mg/L) | 5.2326 | 2.7846 | 1.1016 | 0.85986 | 0.59288 | 0.68238

## Slide 14: RESULTS POST SORPTION CONCENTRATION
Fig 11: 180 hydrochar sample for pH 4
Fig 12: 180 hydrochar sample for pH 7
Chart: Post Sorption concentration (mg/L) pH 4
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Cd 226.502 {449} (Axial) [ppm] | 4.72 | 4.55 | 4.53 | 3.09 | 1.94 | 1.26 | 5.39
Cu 324.754 {104} (Axial) [ppm] | 8.64 | 9.78 | 10.02 | 8.65 | 8.32 | 8.34 | 8.49
Zn 206.200 {464} (Axial) [ppm] | 10.61 | 10.14 | 10.26 | 7.73 | 6.54 | 5.82 | 11.89
Chart: Post Sorption Concentration (mg/L) pH 7
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Cd 226.502 {449} (Axial) [ppm] | 3.49 | 3.25 | 3.69 | 2.77 | 1.7 | 1.24 | 3.77
Cu 324.754 {104} (Axial) [ppm] | 0.68 | 5.46 | 6.79 | 4.82 | 7.91 | 8.33 | 0.01
Zn 206.200 {464} (Axial) [ppm] | 8.29 | 8.18 | 8.56 | 7.19 | 6.9 | 5.54 | 8.27

## Slide 15: RESULTS REMOVAL RATES
Fig 13: 220 hydrochar sample for pH 4
Fig 14: 220 hydrochar sample for pH 7
Chart: Metal removal rate pH 4
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Metal removal rate Cd (%) | 64.2587 | 67.4735 | 64.4478 | 82.7912 | 93.7595 | 95.6505 | -0.41604
Metal removal rate Cu (%) | 3.0206 | 41.5376 | -11.9848 | 44.2658 | 54.2044 | 51.9634 | 14.0602
Metal removal rate Zn (%) | 39.4428 | 49.2072 | 41.2344 | 54.4925 | 61.5695 | 58.2549 | -4.0043
Chart: Metal removal rate pH 7
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Metal removal rate Cd (%) | 76.941 | 50.9202 | 81.172 | 94.2881 | 94.7112 | 95.769 | 14.5335
Metal removal rate Cu (%) | 41.055 | 19.9541 | 13.9908 | 18.8073 | -12.3853 | 0.22936 | 99.5413
Metal removal rate Zn (%) | 62.774 | 36.5079 | 58.1444 | 71.9388 | 57.294 | 59.2782 | 19.3122

## Slide 16: RESULTS SORPTION CAPACITY
Fig 15: 220 hydrochar sample for pH 4
Fig 16: 220 hydrochar sample for pH 7
Chart: Sorption Capacity pH 4
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Sorption Capacity Cd(mg/g) | 0.23786 | 0.12488 | 0.05964 | 0.030646 | 0.021691 | 0.017703
Sorption Capacity Zn (mg/L) | 26.4096 | 15.72 | 5.9933 | 3.3641 | 2.6036 | 1.9925
Sorption Capacity Zn (mg/L) | 9.9144 | 6.6249 | 2.6316 | 1.5055 | 1.092 | 0.81702
Chart: Sorption Capacity pH 7
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Sorption Capacity Cd(mg/g) | 52.334 | 9.316 | 14.4535 | 7.4802 | 4.7094 | 3.836 | 0
Sorption Capacity Zn (mg/L) | 58.3998 | 25.5843 | 12.2812 | 5.0776 | 2.5054 | 2.2205
Sorption Capacity Zn (mg/L) | 18.5436 | 5.0184 | 4.2611 | 2.1512 | 1.048 | 0.87057

## Slide 17: RESULTS POST SORPTION CONCENTRATION
Fig 18: 220 hydrochar sample for pH 7
Fig 17: 220 hydrochar sample for pH 4
Chart: Post sorption concentration (mg/L) pH 4
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Cd 226.502 {449} (Axial) [ppm] | 1.89 | 1.72 | 1.88 | 0.91 | 0.33 | 0.23 | 5.31
Cu 324.754 {104} (Axial) [ppm] | 6.64 | 6 | 6.95 | 5.72 | 4.7 | 4.93 | 8.82
Zn 206.200 {464} (Axial) [ppm] | 6.76 | 5.67 | 6.56 | 5.08 | 4.29 | 4.66 | 11.61
Chart: Post sorption concentration (mg/L) pH 7
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Cd 226.502 {449} (Axial) [ppm] | 1.09 | 2.32 | 0.89 | 0.27 | 0.25 | 0.2 | 4.04
Cu 324.754 {104} (Axial) [ppm] | 2.57 | 3.49 | 3.75 | 3.54 | 4.9 | 4.35 | 0.02
Zn 206.200 {464} (Axial) [ppm] | 3.94 | 6.72 | 4.43 | 2.97 | 4.52 | 4.31 | 8.54

## Slide 18: RESULTS REMOVAL RATE
Fig 19: 260 hydrochar sample for pH 4
Fig 20: 260 hydrochar sample for pH 7
Chart: Removal rates pH 4
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Metal removal rate Cd (%) | 19.583 | 26.6567 | 51.6009 | 94.4155 | 95.1601 | 97.0216 | -0.52122
Metal removal rate Cu (%) | 21.8044 | 22.4209 | 35.9844 | 78.6272 | 76.2639 | 82.3263 | 21.2906
Metal removal rate Zn (%) | 16.324 | 26.4259 | 37.7794 | 88.3783 | 85.7858 | 85.2494 | -5.1314
Chart: Removal rates pH 7
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Metal removal rate Cd (%) | 31.6828 | 44.341 | 40.9903 | 74.4974 | 94.9739 | 96.8354 | 8.2278
Metal removal rate Cu (%) | -83.3631 | -261.3596 | -458.1395 | -291.771 | -78.8909 | -70.8408 | 85.6887
Metal removal rate Zn (%) | 24.5248 | 43.9963 | 36.4859 | 60.0371 | 85.4427 | 86.6481 | 1.7153

## Slide 19: RESULTS SORPTION CAPACITY
Fig 22: 260 hydrochar sample for pH 4
Fig 21: 260 hydrochar sample for pH 4
Chart: Sorption capacity pH 4
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Sorption Capacity Cd(mg/L) | -36.168 | -12.878 | 2.74 | 7.398 | 4.6923 | 3.8908
Sorption Capacity Cu(mg/L) | 18.7854 | 9.6285 | 7.408 | 6.2251 | 3.7777 | 3.254
Sorption Capacity Zn (mg/L) | 1.9584 | 10 | 2.3256 | 2.6622 | 1.6084 | 1.2775
Chart: Sorption capacity pH 7
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Sorption Capacity Cd(mg/L) | -18.358 | 0.137 | -1.1645 | 4.4662 | 4.6751 | 3.8771
Sorption Capacity Cu(mg/L) | 62.487 | 23.4228 | 7.3884 | 4.4173 | 3.93 | 3.1794
Sorption Capacity Zn (mg/L) | 5.6916 | 6.0588 | 2.4097 | 1.7411 | 1.6122 | 1.3097

## Slide 20: RESULTS POST SORPTION CONCENTRATION
Fig 3: 260 hydrochar sample for pH 4
Fig 24: 260 hydrochar sample for pH 7
Chart: Post sorption concentration (mg/L) pH 4
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Cd 226.502 {449} (Axial) [ppm] | 4.32 | 3.94 | 2.6 | 0.3 | 0.26 | 0.16 | 5.4
Cu 324.754 {104} (Axial) [ppm] | 7.61 | 7.55 | 6.23 | 2.08 | 2.31 | 1.72 | 7.66
Zn 206.200 {464} (Axial) [ppm] | 9.36 | 8.23 | 6.96 | 1.3 | 1.59 | 1.65 | 11.76
Chart: Post sorption concentration (mg/L) ph 7
| 0.5 g | 1 g | 2 g | 5 g | 8 g | 10 g | control
Cd 226.502 {449} (Axial) [ppm] | 3.67 | 2.99 | 3.17 | 1.37 | 0.27 | 0.17 | 4.93
Cu 324.754 {104} (Axial) [ppm] | 2.05 | 4.04 | 6.24 | 4.38 | 2 | 1.91 | 0.16
Zn 206.200 {464} (Axial) [ppm] | 8.14 | 6.04 | 6.85 | 4.31 | 1.57 | 1.44 | 10.6

## Slide 21: CONLCUSIONS
Synthetic mine water at pH 4 for 220 hydrochar sample removed most Cd as compared to Cu and Zn.
Precipitation and filtering may explain high metal concentrations after ICP analysis.
Hydrochar sample may contain cd, therefore the variation in concentration after incubation and filtration.

## Slide 22: CONCLUSIONS CLOSING THE LOOP
Fig 25: Summary of the project
Food Waste
Anaerobic Digestion
Hydrochar
Methane
Hydrothermal Processing
Mine Water Treatment
Wastewater from Mining Industry
Treated Water
Land Amendment
Food Production

## Slide 23: REFERENCES
Deliyanni, E.A., Peleka, E.N., Matis, K.A., 2007. Removal of zinc ion from water by sorption onto iron-based nano adsorbent. J. Hazard. Mater. 141, 176–184.
Igwe, J.C., Ogunewe, D.N., Abia, A.A., 2005. Competitive adsorption of Zn (II), Cd (II) and Pb (II) ions from aqueous and non-aqueous solution by maize cob and husk. Afr. J. Biotechnol. 4 (10), 1113– 1116.
Gupta, V.K., Rastogi, A., Saini, V.K., Jain, N., 2006. Biosorption of copper (II) from aqueous solutions by Spirogyra species. J. Colloid In Bishnoi, N.R., Bajaj, M., Sharma, N., Gupta, A., 2003.

## Slide 24
THANK YOU