## Slide 1: Heavy Metal Recovery Using Manganese-Oxidizing Microbes and Recycled Carpet Fiber
Brandy Stewart, Sharon Bone, and Cara Santelli
University of Minnesota

## Slide 2: Project Objective-design bioreactor using Mn-oxidizing fungus
C. Santelli

## Slide 3: Project Objective-design bioreactor using Mn-oxidizing fungus
C. Santelli

## Slide 4: Project Background-Soudan Iron Mine

## Slide 5
Periconia verrucosa

## Slide 6: Experimental Setup
1g polypropylene fiber
100 mL synthetic brine media
500 µM Mn(II)
0.2 mL blended fungal culture
20 µM (Ni(II), Co(II), Cu(II))
Day 1-initial conditions
No fiber Carpet fiber

## Slide 7: Experimental Setup
1g polypropylene fiber
100 mL synthetic brine media
500 µM Mn(II)
0.2 mL blended fungal culture
20 µM (Ni(II), Co(II), Cu(II))
Periconia verrucosa
Day 1-initial conditions
No fiber Carpet fiber
Mn(II) (aq) Mn (III/IV) solid

## Slide 8: Results - Carpet Fiber Impact
Day 7 – Mnoxide/fungal biofilm with carpet fiber Day 7 – Mnoxide/fungal biofilm with no carpet fiber
Carpet fiber visibly increases biomass and Mnoxide amount

## Slide 9
Fungal culture without Mn Fungal culture with Mn oxide precipitates

## Slide 10
Fungal culture with Mn oxide precipitates

## Slide 12
10 µm
Complex, dense network of fungal material and biominerals

## Slide 14
Soluble metal concentrations decrease over time

## Slide 15
Presence of carpet fiber enhances metal removal

## Slide 16
Soluble Mn concentration decreases over time

## Slide 17
Soluble Mn concentration decreases over time

## Slide 18
Soluble metals decrease over time

## Slide 19
Carpet fibers enchance metal removal

## Slide 20
Mnoxide
Fungi
Carpet Fiber

## Slide 21
Soluble Mn concentration decreases over time

## Slide 22
Soluble metals decrease

## Slide 23
Carpet fibers enchance metal removal and pH buffering helps removal

## Slide 24
Carpet Fiber
Fungal Biomass

## Slide 25
Proportion of metal associated with Mnoxide phase depends on metal

## Slide 26
Results – Fungal biomineral interaction
Fungi
Mnoxide material

## Slide 29
500 um
500 um
Cu
Mn
Trace metals co-located with Mn oxides
Results – Fungal metal association

## Slide 30
Xray fluorescence map of fungal biomass and mixed metal
precipitation showing co-location of Mn with Cu, Co, Ni
Co
Mn

## Slide 31
Co
Mn
Ni
Cu

## Slide 32: Conclusions-what we know so far
Mn oxidizing fungi sequesters Co, Ni, Cu with Mn biomineral
Carpet fibers increase metal uptake
Fungus grows well in salty brine media

## Slide 33: Ongoing work-Soudan Mine Water
Elevated levels of Cu and Ni
Can this be treated with fungal system?

## Slide 34: Ongoing work-Soudan Mine Water
Elevated levels of Cu and Ni
Can this be treated with fungal system?

## Slide 35: Acknowledgements
Santelli Lab
Soudan Mine
Stanford Synchrotron Radiation Laboratory
Industrial Partners
  Clearwater Biologic
Funding Source
  MnDrive: Minnesota’s Discovery, Research, and InnoVation Economy

## Slide 36
Mn K-edge EXAFS
Carpet Fiber is not impacting local manganese coordination chemistry

## Slide 38
Soudan pics, new show copper
Mention industrial partner
Tem pictures
New graph results, include bar charts
Explain what we are looking at with SEM, maybe add an image
Explain Mn chemistry or exclude that slide
Add that we are including mine water now and working
Add pictures of that if we have

## Slide 40
Chart: Time (d)
| 2 | 4 | 11 | 35 | 36 | 39 | 52
Fiber, Co+Cu | 445.5 | 434.8756 | 315.871 | 170.2827 | 135.2631 | 116.4191 | 2.2246
no Fiber, Co+Cu | 447.5056 | 443.0176 | 348.4637 | 229.5311 | 237.5676 | 271.0983 | 285.7266
Fiber, Cu | 435.2436 | 429.6943 | 333.4145 | 153.5272 | 141.6429 | 150.422 | 17.1678
no Fiber, Cu | 453.2454 | 445.2078 | 353.9921 | 235.3388 | 251.9399 | 280.1534 | 287.6264
Fiber, Co+Cu+Zn | 450.5433 | 432.6365 | 330.8664 | 137.6425 | 125.3607 | 115.7396 | 7.2455
no Fiber, Co+Cu+Ni | 443.9983 | 441.8711 | 344.8027 | 243.9297 | 253.613 | 287.6421 | 330.4751

## Slide 42
Chart: Time (d)
| 0 | 1 | 3 | 14
Cu+Fiber | 18.2781 | 10.3454 | 8.1014 | 4.5992
Cu no fiber | 17.2139 | 8.942 | 10.0963 | 10.1067
Co+Fiber | 24.4793 | 8.9674 | 3.9502 | 0.5906
Co no Fiber | 23.6442 | 13.5653 | 10.4757 | 9.4675
Ni+Fiber | 20.3635 | 13.9019 | 11.733 | 3.6045
Ni no Fiber | 20.6189 | 18.5475 | 18.5584 | 18.2666